List of copper ores
Following is a list of minerals that serve as copper ores in the copper mining process:
	Name
	Formula
	 % Copper
when pure

	[image: Min chalcopyrite.jpg]
Chalcopyrite
	CuFeS2
	34.5

	[image: Chalcocite.jpg]
Chalcocite
	Cu2S
	79.8

	[image: Covellite-USA.jpg]
Covellite
	CuS
	66.5

	[image: Bornite.jpg]
Bornite
	2Cu2S·CuS·FeS
	63.3

	[image: Tetraedrite.jpg]
Tetrahedrite
	Cu3SbS3 + x(Fe,Zn)6Sb2S9
	32–45

	[image: Digenite.jpg]
Digenite
	Cu9S5
	78.1

	[image: Malachite Macro 43.jpg]
Malachite
	CuCO3•Cu(OH)2
	57.7

	[image: Azuritechessy.jpg]
Azurite
	2CuCO3·Cu(OH)2
	55.1

	[image: Cuprite.jpg]
Cuprite
	Cu2O
	88.8

	[image: Chrysocolla USA.jpg]
Chrysocolla
	CuO·SiO2·2H2O
	37.9

	[image: Tennantite2.jpg]
Tennantite
	Cu12As4S13
	51.6

	Copper-bearing minerals[1]
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